Peculiarities of the photoluminescence line shape in Ga(N,As,P)/GaP: Experiment and Monte Carlo simulations
V. Valkovskii
Prof. S. D. Baranovskii
vitalii.valkovskii@physik.uni-marburg.de
GRK Seminar 2017, Kunze-Hof, Stadland, 2017

---
Monte Carlo studies
Computer simulations of disordered materials properties:
- Charge Transport properties
- Optical properties
Ga(N,As,P)/GaP PL

---
Outline
- Intro
- Baranovskii – Eichmann – Thomas(BET) model
- Modified BET – model : Two scales of disorder
- Alternative approach : Complex DOS and T-dependent non-radiative recombination
- Conclusions

---
Disorder-induced localized states
Tale of localized states (LS) due to disorder:
E_g
DOS

---
Peculiarities of PL in disordered material
 (a) Schematic shapes of the PL spectra;
 (b) temperature-dependent PL peak position;
 (c) PL linewidth;
 Green solid line – low excitation
 Red doted line – high excitation

---
Experimental measurements
PL Spectra:
PL Features:
 Karcher C, Jandieri K, Kunert B, Fritz R, Zimprich M,Volz K, Stolz W, Gebhard F, Baranovskii S D and Heimbrodt W 2010 Phys. Rev. B 82 245309

---
BET - model
Assumptions:
- Traps distributed randomly in energy and coordinates;
- No correlations between energy and spatial positions of traps are assumed;
- Electrons and holes are coupled in form of excitons.
Processes:
- Capture to localized states (LS);
- Activation to extended states;
- Hopping transitions between LS;
- Recombination;
%nu_i = %nu_0 exp left ( {-E_i} over {kT} right )
%nu_ij = %nu_0 exp left ( {-2R_ij} over {a} - {E_j - E_i + lline E_j - E_i rline } over {2kT} right )
Dimensionless parameters:
{E_0} over {kT}
Na^{2}
%nu_0%tau_0
 Baranovskii S D, Eichmann R and Thomas P 1998 Phys.Rev. B 5813081

---
BET - model
KMC Simulation algorithm:
- Step 1: Generate LS’s ;
- Step 2: Set particle to random site;
- Step 3: Throw random number to select next event;
- Step 4: Throw random number to generate event’s time;
- Repeat Steps 3-4 until recombination.
Hopping
Activation
1
0
. . .
%DELTA t_i = -ln(x) %nu_i ^{-1}
Recombi-
nation

---
BET - model
Successfully applied to:
- Quantum wells:
  GaInNAs/GaNAs, InGaN/GaN
- Quantum dost:
  InAs/GaAs
- Bulk materials:
  GaP(N)
Key feature:
Relations between energy scale of disorder(E) and temperature maximums (T1 and T2)of PL Stokes Shift / FWHM.
Feature	Relation to E/k
T1 (Stokes Shift max)	~ (0.7 – 0.8)
T2 (FWHM max)	~ (1.1 – 1.2)
FWHM (at low T)	~ 2.5
 Rubel O, Galluppi M, Baranovskii S D, Volz K, Geelhaar, L, Riechert H, Thomas P and Stolz W 2005 J. Appl. Phys.98 063518
 Dawson P, Rubel O, Baranovskii S D, Pierz K, Thomas P and Goebel E O 2005 Phys. Rev. B 72 235301
 Dawson P, Goebel E O, Pierz K, Rubel O, Baranovskii S D and Thomas P 2007 Phys. Stat. Sol. b 244 2803

---
Problems of BET – model for Ga(N,As,P)
Problem:
Relations between PL features
and energy parameter of disorder
doesn’t work!
 Karcher C, Jandieri K, Kunert B, Fritz R, Zimprich M,Volz K, Stolz W, Gebhard F, Baranovskii S D and Heimbrodt W 2010 Phys. Rev. B 82 245309

---
Modified BET – model: Two scales of disorder
DOS for double-scale of disorder:
Simulated spectrum:
G(E) = {N_0} over { %varepsilon_0 - E_0 } left [ exp left ( {E} over {%varepsilon_0} right ) - exp left ( {E} over {E_0} right ) right ]
 Karcher C, Jandieri K, Kunert B, Fritz R, Zimprich M,Volz K, Stolz W, Gebhard F, Baranovskii S D and Heimbrodt W 2010 Phys. Rev. B 82 245309

---
Modified BET – model. Two scales of disorder
Experimental results and simulation:
 Karcher C, Jandieri K, Kunert B, Fritz R, Zimprich M,Volz K, Stolz W, Gebhard F, Baranovskii S D and Heimbrodt W 2010 Phys. Rev. B 82 245309

---
Ga(N,As,P) PL FWHM vs pump
Experimental result: At low temperatures FWHM strongly decreases along with the increase of the Peak Energy, when increasing the excitation power
Similar behavior reported for GaAsBi/GaAS:
Mazur Y I et al 2013 J. Phys. D: Appl. Phys. 46 065306

---
Modified BET – model: Complex DOS
Complex DOS:
Simulation results:
g(E) = A_0 exp left ( -{E} over {E_0} right ) + A_1 exp left ( {-( E - E_1 )} over { %sigma_1 } right )
 Valkovskii V V, Shakfa M K, Jandieri K, Ludewig P, Volz K, Stolz W, Koch M and Baranovskii S D , 2017 J. Phys. D: Appl. Phys 50 025105

---
Experimental measurements
PL Spectra:
PL Features:
 Karcher C, Jandieri K, Kunert B, Fritz R, Zimprich M,Volz K, Stolz W, Gebhard F, Baranovskii S D and Heimbrodt W 2010 Phys. Rev. B 82 245309

---
Modified BET – model. Two types of LS
Assumptions:
- Many particle system;
- Complex DOS given by:
  ;
- Two types of the LS;
- Strong temperature dependence of non-radiative recombination;
- New parameter – ratio of non-radiative recombination rates .
g(E) = A_0 exp left ( -{E} over {E_0} right ) + A_1 exp left ( {-( E - E_1 )} over { %sigma_1 } right )
%tau_{nr,1} / %tau_{nr,1}

---
Modified BET – model. Two types of LS
Simulation results :

---
Conclusions
- We have studied PL features of Ga(N,As,P) quantum wells using Kinetic Monte Carlo method;
- Principal problems of the original BET – model has been revealed;
- The original model has been refined, assuming the following:
  - Two types of LS with non-monotonous (exponential-plus-Gaussian) DOS;
  - Strongly different temperature dependencies of non-radiative recombination rates at LS type-I and LS type-II